Supplementary Table XII

| A | Ascending Aorta |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | WT VEH |  |  | MFS VEH |  |  | MFS BAC |  |  |
|  | n | = | 5 | n | = | 4 | n | = | 6 |
| Unloaded Dimensions |  |  |  |  |  |  |  |  |  |
| Wall Thickness, H (μm) | 112 | ± | 1.8 | 156 | ± | 4.1* | 144 | ± | 7.4* |
| Inner Diameter, 2A (μm) | 871 | ± | 33 | 1661 | ± | 142* | 1279 | ± | 121*,# |
| Dimensions at Diastolic Pressure P (mmHg) | P | = | 97 | P | = | 77 | P | = | 64 |
| Wall Thickness, h (μm) | 38 | ± | 1.0 | 68 | ± | 2.9* | 60 | ± | 4.6* |
| Inner Diameter, 2a (µm) | 1613 | ± | 60.3 | 2487 | ± | 161.5* | 2039 | ± | 160.2*,# |
| Dimensions at Systolic Pressure P (mmHg) | P | = | 127 | P | = | 110 | P | = | 82 |
| Wall Thickness, h (μm) | 36 | ± | 0.9 | 66 | ± | 2.8* | 58 | ± | 4.8* |
| Inner Diameter, 2a (µm) | 1729 | ± | 63.8 | 2558 | ± | 167.5* | 2117 | ± | 154.5*,# |
| Distensibility (1/MPa) | 18.01 | ± | 0.52 | 6.51 | ± | 0.35* | 16.81 | ± | 3.37# |
| Additional Metrics at Systolic Pressure |  |  |  |  |  |  |  |  |  |
| In vivo Axial Stretch, λz | 1.75 | ± | 0.03 | 1.62 | ± | 0.02 | 1.65 | ± | 0.06 |
| Circumferential Cauchy Stress, σθ (kPa) | 413 | ± | 20.9 | 282 | ± | 10.2* | 203 | ± | 11.4*,# |
| Axial Cauchy Stress, σz (kPa) | 332 | ± | 10.8 | 180 | ± | 5.9* | 166 | ± | 13.7* |
| Circumferential Linearized Material Stiffness,Cθθθθ (MPa) | 2.89 | ± | 0.27 | 5.40 | ± | 0.21* | 2.17 | ± | 0.28# |
| Axial Linearized Material Stiffness, Czzzz (MPa) | 1.70 | ± | 0.09 | 1.35 | ± | 0.08* | 1.09 | ± | 0.05* |
| Stored Strain Energy Density, W (kPa) | 107 | ± | 4.9 | 37 | ± | 2.1* | 42 | ± | 6.1* |

Means ± standard errors of biaxial biomechanical metrics of the ascending aorta. * and #, p<0.05 with regard to WT vs. VEH and MFS vs. VEH groups, respectively.

| B | Ascending Aorta |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | WT VEH |  |  | MFS VEH |  |  | MFS BAC |  |  |
|  | n | = | 5 | n | = | 4 | n | = | 6 |
| Dimensions at Fixed Pressure P (mmHg) | P | = | 100 | P | = | 100 | P | = | 100 |
| Wall Thickness, h (μm) | 38 | ± | 1.0 | 67 | ± | 2.8* | 56 | ± | 4.8* |
| Inner Diameter, 2a (µm) | 1627 | ± | 60.9 | 2542 | ± | 166.0* | 2168 | ± | 151.7*,# |
| Additional Metrics at Fixed Pressure |  |  |  |  |  |  |  |  |  |
| Circumferential Cauchy Stress, σθ (kPa) | 289 | ± | 14.8 | 253 | ± | 9.0 | 260 | ± | 15.4 |
| Axial Cauchy Stress, σz (kPa) | 282 | ± | 10.1 | 172 | ± | 4.9* | 192 | ± | 16.2* |
| Circumferential Linearized Material Stiffness,Cθθθθ (MPa) | 1.65 | ± | 0.08 | 4.31 | ± | 0.12* | 3.22 | ± | 0.32*,# |
| Axial Linearized Material Stiffness, Czzzz (MPa) | 1.37 | ± | 0.07 | 1.26 | ± | 0.06 | 1.32 | ± | 0.07 |
| Stored Strain Energy Density, W (kPa) | 87 | ± | 4.0 | 36 | ± | 2.0* | 47 | ± | 7.1* |

Means ± standard errors of biaxial biomechanical metrics of the ascending aorta evaluated at a common pressure of 100 mmHg. * and #, p<0.05 with regard to WT vs. VEH

and MFS vs. VEH groups, respectively.